August 4, 2004

Grabber Construction Products			                        Laboratory No.: V488

20 West Main Street Court						Client No.: WAG630

Alpine, Utah 84004							                 Page 1 of 2

Subject: Lateral Resistance on Deckmaster Hidden Bracket secured to EPI Hardwood

As requested Testing Engineers, Inc. (TEI) performed the subject testing on the submitted samples. Testing was performed on 60 kip Instron model # 4486 s/n 113113J  (calibration traceable to N.I.S.T.).

# TEST SPECIMEN DESCRIPTION   (Lateral Resistance Test Assemblies)

The shear test consisted of one (1) EPI hardwood 1” x 6” x 12” long and one (1) Deckmaster Hidden Bracket, and one (1) Deckmaster screw.  Each test assembly was secured together with a single test screw from the Deckmaster bracket into the EPI wood.  Shear testing was conducted on 10 x 1” and 10 x 1-1/4” Deckmaster Screws.

LATERAL RESISTANCE

The EPI hardwood was secured into the testing machine using a pin and clevis and the Deckmaster bracket was secured in the lower v-jaw.   An axial tensile load was applied at a gradual rate until failure.  Simultaneous values of load and differential movement were recorded.  Test results and sample identification are presented in Tables 1 and 2.

Table 1

| Deckmaster 10 x 1¼ " screw DM125G |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Loads (lbs) at Specified displacements (inches) |  |  |  |  |  |  |  |
| Sample # | 0.01 | 0.015 | 0.05 | 0.100 | 0.200 | 0.300 | Ultimate Load | Failure Mode |
| 1 | 55 | 64 | 119 | 225 | 496 | 762 | 783 | Screw sheared |
| 2 | 23 | 26 | 47 | 111 | 206 | 285 | 564 | Screw sheared |
| 3 | 21 | 35 | 60 | 156 | 453 | 646 | 656 | Screw sheared |
| Average | 33 | 42 | 75 | 164 | 385 | 564 | 668 |  |
|  |  |  |  | Table 2 |  |  |  |  |
| Deckmaster 10 x 1" screw DM100G |  |  |  |  |  |  |  |  |
|  | Loads (lbs) at Specified displacements (inches) |  |  |  |  |  |  |  |
| Sample # | 0.01 | 0.015 | 0.05 | 0.100 | 0.200 | 0.300 | Ultimate Load | Failure Mode |
| 1 | 5 | 10 | 60 | 161 | 460 | 746 | 792 | Screw sheared |
| 2 | 7 | 21 | 60 | 139 | 422 | 580 | 590 | Screw sheared |
| 3 | 6 | 10 | 69 | 169 | 511 |  | 722 | Screw sheared |
| Average | 6 | 14 | 63 | 156 | 464 | 663 | 701 |  |

Sincerely,

TESTING ENGINEERING, INC.

Jack A. Snow

Material Testing Laboratory Technician

The results presented in this report relate only to the items tested. This report can only be reproduced in its entirety unless written permission from TEI is obtained.

Deckmaster notes: The test results are for a single fastener. Per Deckmaster installation instructions and building codes, a minimum of two (2) screws per board, per joist are the minimum requirement.

System values are described in the Uniform Uplift Values in lbs/sf and average over 1,000 lbs/sf using redwood.

Updated 07/28/06